## Slide 1: JCTCollege of Engineering & Technology Pichanur, Coimbatore- 641105.
High Volatge Engineering
Faculty Name: Dr.K.Geetha
Designation : Professor,
Year /Sem : IV/VII
Dept : EEE

## Slide 2: UNIT - II
ELECTRICAL BREAKDOWN IN GASES, SOLIDS AND LIQUIDS.

## Slide 3: GASEOUS BREAKDOWN IN UNIFORM FIELDS
In uniform fields, the Townsend's criterion for breakdown in electropositive gases is given by the following equation,
where the coefficients α and γ are functions of E/p and are given as follows

## Slide 4: GASEOUS BREAKDOWN IN UNIFORM FIELDS
where E0 is the applied electric field, and p the gas pressure. In a uniform field electrode system of gap distance d,
Ub is the breakdown voltage and Eb the corresponding field intensity. Eb is equal to the electric strength of the dielectric under given conditions. When the applied field intensity E0 = Eb

## Slide 5: GASEOUS BREAKDOWN IN UNIFORM FIELDS

## Slide 6: BREAKDOWN IN LIQUID DIELECTRICS
,
This is known as Paschen's law. The scientist,
A very large number of external factors affect the breakdown strength of liquid dielectrics. For example, electrode configuration, their material, size and surface finish, the type of voltage, its period of application and magnitude, the temperature, pressure, purification of the liquid and its ageing condition.

## Slide 7: BREAKDOWN IN LIQUID DIELECTRICS
,
This is known as Paschen's law. The scientist,
Dissolved water, gas or the presence of any other form of contamination and sludge also affect the breakdown strength considerably. It is, therefore, not possible to describe the breakdown mechanism by a single theoretical analysis which may take into account all known observed factors affecting the breakdown.

## Slide 8: CORONA DISCHARGE
The field is non-uniform, an increase in voltage will first cause a discharge in the gas to appear at points with highest electric field intensity, namely at sharp points or where the electrodes are curved or on transmission lines. This form of discharge is called a corona discharge and can be observed as a bluish luminescence.

## Slide 9: CORONA DISCHARGE
This is accompanied by a hissing noise.
The air surrounding the corona region becomes converted into ozone.
It is responsible for considerable loss of power from high voltage transmission lines,
It leads to the deterioration of insulation due to the combined action of the bombardment of ions and of the chemical compounds formed during discharges.
It also gives rise to radio interference.

## Slide 10: BREAKDOWN IN NON-UNIFORM FIELDS
The breakdown voltages were also observed to depend on humidity in air.
In rod gaps the fields are non-uniform.
In the case of sphere gaps the field is uniform
In sphere gaps, the breakdo0wn voltage do not depend on humidity and are also independent of the voltage waveform
The formative time lag is quite small (~0.5µs) even with 5% over-voltage.

## Slide 11: VACUUM BREAKDOWN
It can be broadly divided into following categories
Particle exchange mechanism.
Field emission mechanism.
Clump theory

## Slide 12: CONDUCTION & BREAKDOWN IN COMMERCIAL LIQUIDS
Suspended particle mechanism
Cavitation and bubble mechanism
Stressed oil volume mechanism
Thermal mechanism of breakdown

## Slide 13: BREAKDOWN IN SOLID DIELECTRICS
Chemical & electrochemical deterioration & breakdown
Breakdown due to treeing and tracking
Breakdown due to internal discharges

## Slide 14: BREAKDOWN IN COMPOSITE DIELECTRICS
Mechanism of breakdown in composite dielectric
1. Short-term breakdown
2. Long-term breakdown

## Slide 15: CONDUCTION & BREAKDOWN IN PURE LIQUIDS
Low electric fields less than 1 kV/cm are applied, conductivities of 10-18–10-20 mho/cm are obtained.
These are due to impurities remaining after purification
When the fields are high the currents not only increase rapidly.